SRI Grease OEM NLGI 2

Polyurea Grease

Texaco's SRI Grease OEM NLGI 2  is a top quality polyurea thickened grease manufactured with highly refined paraffinic oil.  It has a blue-green colour and a buttery texture.  The grease is oxidation inhibited to provide outstanding stability at high temperatures.  A high level of rust inhibitors protects bearings from corrosion in wet and salty environments.  SRI Grease OEM NLGI 2 is compatible with other products that are commonly used in anti-friction bearings such as sodium and lithium based greases.

Recommendations for Use

SRI Grease OEM NLGI 2 can be used in automotive and industrial applications, particularly where the operating speeds are high, temperatures are in the order of 150°C, or where there is the likelihood of fresh or salt water ingress into the bearings.  It can be applied successfully at temperatures down to -30°C.  SRI Grease OEM NLGI 2 gives outstanding service especially in equipment operating intermittently under severe conditions.  The ASTM D3336 test shows that the life of a 204-K bearing lubricated with SRI Grease OEM NLGI 2 and operating at 150 °C and 10000 rpm is about 3000 hours.  This is nearly 10 times the life possible when using a conventional lithium grease and about three times that when using a sodium greases.  Regarding nuclear radiation resistance, testing has indicated that SRI Grease OEM NLGI 2 can withstand at least 2x108 rads and still provide effective lubrication and rust protection.  SRI Grease OEM NLGI 2 has been authorised by the USDA for use in federally inspected meat and poultry plants as an H2 lubricant with no food contact.  Applications where perforrnance is proven include:

Antifriction bearings operating at  high speeds (10000 rpm and greater)

Bearings on automotive alternators, water purnps and starters

Bearings on air conditioning units

Electric motor bearings operating under moist conditions

High speed fans and blowers

Health and Safety

SRI Grease OEM NLGI 2 has been formulated to the highest safety standards and is unlikely to present any significant health and safety hazards when used properly in the recommended application and when good standards of industrial and personal hygiene are maintained.  However, should eye contact occur, flush for a minimurn of 15 minutes with clean water.  A comprehensive Materials Safety Data Sheet is available on request and is supplied as a matter of course to purchasers of this product.

Typical Data

| Usable temperature range °C | -30 to +175 |
| --- | --- |
| NLGI Grade | 2 |
| Appearance | Blue-green, buttery |
| Dropping point °C | 243 |
| Penetration |  |
| worked | 280 |
| unworked | 195 |
| Rusting test, 24 hrs at 52 °C |  |
| ASTM D 1743 |  |
| (distilled water + 5% synthetic sea water) | 1 (no rust) |
| IP220 | 0 (no rust) |
| Base oil characteristics |  |
| Kinematic viscosity |  |
| cSt at 40 °C | 99 |
| cSt at 100 °C | 11.0 |
| Viscosity index | 95 |
| Pour point, °C | -15 |
| Flash point, °C | 260 |
| DIN Classification | K2N-30 |
| Speed rating, ndm | >500,000 |

Issued Mar. 1996

For further information, please contact your local Area Manager, or stockist.