High temperature and

Long life grease

## ＭＵＬＴＥＭＰ　ＥＴ－Ｋ

MULTEMP ET-K is designed especially for use in rolling bearings of automobile electrical  equipment such as alternators and electromagnetic clutches.  MULTEMP ET-K  has long  performance life under high temperature and high speed conditions, together with excellent rust preventive properties.

### Typical analyses

Usage temperature range －40℃ ⇔ 200℃

| Test item |  | Test method | MULTEMP ET－Ｋ |
| --- | --- | --- | --- |
| # Thickener |  | ――――― | aromatic diurea |
| Base oil |  | ――――― | ether－based synthetic oil ＋ polyolester |
| Base oil kinematic viscosity (40℃) ㎜2/ｓ |  | ASTM D 445 | 95.1 |
| # Appearance |  | ――――― | light brown, buttery |
| # Worked penetration |  | ASTM D 217 | 300 |
| Dropping point ℃ |  | ASTM D 566 | 230 |
| Oil separation mass% | 100℃,24h | FTMS 791C－321 Mod. | 1.0 |
|  | 150℃,24h |  | 1.6 |
| Low－temperature torque N・㎝ | (－30℃) Starting torque Running torque | ASTM D 1478－63 | 33 9.6 |
| Corrosion preventive properties (52℃,48h) |  | ASTM D 1743－73 | # 1 |

01/2

KYODO YUSHI Co., LTD.

2－16－7，Ginza,Chuo－ku, Tokyo 104-0061,Japan

Phone:（03）3543－5814　Facsimile:（03）3545－6259