Wide－temperature range

rolling bearing grease

## ＭＵＬＴＥＭＰ　ＬＲＬ　№３

MULTEMP LRL No. 3 consists of special synthetic oil having excellent thermal stability at high temperatures, highly refined lithium soap and strictly selected antioxidant and rust inhibitor.  MULTEMP LRL No. 3 will achieve the desired performance life under high-temperature conditions.

### Typical  analyses

Usage temperature range －50℃ ⇔ 150℃

| Test item |  | Test method | # MULTEMP LRL №３ |
| --- | --- | --- | --- |
| # Thickener |  | ――――― | #### lithium soap |
| Base oil |  | ――――― | polyolester |
| Base oil kinematic viscosity (40℃) ㎜2/ｓ |  | ASTM D 445 | 30.0 |
| # Appearance |  | ――――― | peach white, buttery |
| Worked penetration |  | ASTM D 217 | 235 |
| Dropping point ℃ |  | ASTM D 566 | 205 |
| Copper strip corrosion (100℃,24h) |  | ASTM D 4048 | pass |
| Evaporation loss (99℃, 22h) mass% |  | ASTM D 972 | 0.30 |
| Oil separation (100℃,24h) mass% |  | FTMS 791C－321 Mod. | 1.9 |
| Oxidation stability (99℃,100h) kPa |  | ASTM D 942 | 20 |
| # Working stability |  | FTMS 791C－313 | 320 |
| Water washout (38℃,1h) mass% |  | ASTM D 1264 | 1.0 |
| Low－temperature torque N・㎝ | (－40℃) Starting torque Running torque | ASTM D 1478－63 | 21 7.8 |
| Corrosion preventive properties (52℃,48h) |  | ASTM D 1743－73 | # 1 |

01/3